Supporting  Information

Fig. S1.   Transmittance (T %) at 500 nm of aqueous SDS – NaCl solutions plotted against the added amount of the hydrophobic monomer.  Data obtained for the hydrophobe C18A are given.  SDS = 7 w/v %.  Temperature = 35oC.  NaCl concentrations are indicated.

Fig. S2. G’ (symbols) and tan  (curves) of the reaction solutions during the micellar copolymerization of AAm and the hydrophobes (CxR) shown as a function of the reaction time.   = 6.3 rad/s, o  = 0.01.

Fig. S3.  G’ (filled symbols) and G’’ (open symbols) of the physical gels shown as a function of angular frequency  measured after 3h of reaction time. o = 0.01. Type of the hydrophobe indicated.

Fig. S4. Frequency dependencies of tan  for the physical gels formed with various hydrophobes indicates.  o  = 0.01.

Fig. S5.  Stress-strain curves of the physical gels under compression as the dependence of true true stress on the deformation ratio .  The type of the hydrophobes indicated.

Fig. S6. (A): Three successive loading / unloading cycles for gel samples formed using different hydrophobic monomers indicated.  Maximum load = 5 N.  (B): Hysteresis energy Uhys of the physical gels shown as a function of the maximum load.

Fig. S7.  (A, B):  G’ (filled symbols) and  G’’ (open symbols) of gels with (A) and without SDS (B) shown as a function of angular frequency .  o  = 0.01.  The type of the hydrophobes indicated.