FLEXURAL-TORSIONAL COUPLED VIBRATION ANALYSIS OF A THIN-WALLED CLOSED SECTION COMPOSITE TIMOSHENKO BEAM BY USING THE DIFFERENTIAL TRANSFORM METHOD

Metin O. Kaya and Özge Özdemir

Istanbul Technical University, Faculty of Aeronautics and Astronautics, 34469, Maslak, Istanbul, Turkey

Abstract. In this study, a new mathematical technique called the Differential Transform Method (DTM) is introduced to analyse the free undamped vibration of an axially loaded, thin-walled closed section composite Timoshenko beam including the material coupling between the bending and torsional modes of deformation, which is usually present in laminated composite beams due to ply orientation. The partial differential equations of motion are derived applying the Hamilton’s principle and solved using DTM. Natural frequencies are calculated, related graphics and the mode shapes are plotted. The effects of the bending-torsion coupling and the axial force are investigated and the results are compared with the studies in literature.

- Introduction

Figure 1. Configuration of an axially

loaded composite Timoshenko beam

A composite thin-walled beam with length , cross sectional dimension  and wall thickness  is shown in Fig.1. The geometric dimensions are assumed to be  so the terms related to the warping stiffness and the warping inertia are small enough to be neglected.

The bending motion in the  direction, the torsional rotation about the  axis and the rotation of the cross section due to bending alone are represented by ,  and , respectively. A constant axial force  acts through the centroid of the cross section which coincides with the  axis.  is positive when it is compressive as in Fig.1.

- Formulation

The governing undamped partial differential equations of motion are derived for the free vibration analysis of the beam model represented by Fig.1. After the application of the Hamilton’s principle, the following equations of motion are obtained as follows

(1)

(2)

(3)

Here,  is the mass per unit length;  is the polar mass moment of inertia;  and  are flexure–torsion coupling rigidity and shear rigidity of the beam, respectively.

The boundary conditions at  and  for Eqs. (1)-(3) are as follows

(4)

(5)

(6)

A sinusoidal variation of ,  and  with a circular natural frequency  is assumed and the functions are approximated as

,	,				              (7)

The following nondimensional parameters can be used to simplify the equations of motion

,	,	,	,			              (8)

Substituting Eqs.(7) and (8) into Eqs.(4)-(5), the dimensionless equations of motion are

obtained as follows

(9)

(10)

(11)

where the dimensionless coefficients are

,					              (12)

- The Differential Transform Method

The differential transform method is a transformation technique based on the Taylor series expansion and is used to obtain analytical solutions of the differential equations. In this method, certain transformation rules are applied and the governing differential equations and the boundary conditions of the system are transformed into a set of algebraic equations in terms of the differential transforms of the original functions and the solution of these algebraic equations gives the desired solution of the problem.

A function , which is analytic in a domain D, can be represented by a power series with a center at , any point in D. The differential transform of the function is given by

(13)

where  is the original function and  is the transformed function. The inverse transformation is defined as

(14)

Combining Eqs. (13) and (14) and expressing  by a finite series, we get

(15)

Here, the value of  depends on the convergence of the natural frequencies [1]. Theorems that are frequently used in the transformation procedure are introduced in Table 1 and theorems that are used for boundary conditions are introduced in Table 2 [2].

Table 1. Basic theorems of DTM

| Original Function | DTM |
| --- | --- |

Table 2. DTM theorems for boundary conditions

| Boundary Condition | Transformed B.C. | Boundary Condition | Transformed B.C. |
| --- | --- | --- | --- |

- Formulation with DTM

In the solution step, the differential transform method is applied to Eqs.(9)-(11). Here we quit using the bar symbol on , , and instead, we use , , .

(16)

(17)

(18)

Applying DTM to Eqs. (4)–(6), the boundary conditions are given as follows

at           						   (19)

at            				   (20)

(21)

(22)

- Results and Discussion

In order to validate the computed results, an illustrative example, taken from Ref [3], is solved and the results are compared with the ones in the same reference. Additionally, the mode shapes of the beam are plotted.

Variation of the first five natural frequencies (coupled and uncoupled) of the above example with respect to the axial force is introduced in Table 3 and compared with the results of Ref. [3] and [4]. Here, it is noticed that the natural frequencies decrease as the axial force varies from tension  to compression . Additionally,it is seen that the coupled natural frequencies are lower than the uncoupled ones. However, the fourth natural frequency becomes less when the bending-torsion coupling is ignored.

Table3. Natural frequencies with respect to the axial force

| Natural Frequencies |
| --- |
| Present | Ref. [4] | Present§ | Ref.[3]§ | Present | Present§ | Ref.[3]§ | Present | Ref.[4] | Present§ | Ref.[3]§ |
| 40.975 | 40.97 | 37.106 | 37.1 | 35.283 | 30.747 | 30.75 | 28.064 | 28.06 | 21.987 | 21.99 |
| 224.259 | 224.25 | 197.672 | 197.7 | 217.341 | 189.779 | 189.8 | 210.162 | 210.16 | 181.495 | 181.5 |
| 598.668 | 598.66 | 525.665 | 525.6 | 592.626 | 518.791 | 518.8 | 586.519 | 586.51 | 511.818 | 511.9 |
| 647.595 | 647.59 | 648.495 | 648.6 | 647.411 | 648.269 | 648.3 | 647.228 | 647.22 | 648.047 | 648 |
| 1125.71 | 1125.71 | 992.878 | - | 1119.85 | 986.199 | - | 1113.950 | 1113.95 | 979.473 | - |

§ Natural frequencies with coupling

The effects of the axial force  and the Timoshenko effect, , on the first four natural frequencies are introduced in Figs. 2(a-d). When Fig. 2 is examined, it is noticed that the natural frequencies decrease with the increasing rotary inertia parameter, , because Timoshenko effect decreases the natural frequencies and this effect is more dominant on higher modes as expected. Additionally, since the fourth mode is torsion, the Timoshenko effect makes a slight change in the fourth natural frequency value.

Figure 2. Effect of the Timoshenko effect on the first four natural frequencies (           , Timoshenko ;

, Euler)

Mode shapes of the considered beam under the effect of the compressive axial force () are introduced with bending-torsion coupling in Figs. 5(a-d). When these figures are considered, it can be noticed that the first three normal modes are bending modes while the fourth normal mode is the fundamental torsion mode.

Figure 5. The first four normal mode shapes of the composite beam with bending-torsion coupling

(          ,;           , ;           ,)

References

S.H. Ho and C.K. Chen, Analysis of General Elastically End Restrained Non-Uniform Beams Using Differential Transform, Applied Mathematical Modeling 22 (1998) 219-234

Özdemir Ö, Kaya MO, Flapwise Bending Vibration Analysis of a Rotating Tapered Cantilevered Bernoulli-Euler Beam by Differential Transform Method, Journal of Sound and Vibration (In Press).

J.R. Banerjee, Free vibration of axially loaded composite Timoshenko beams using the dynamic stiffness matrix method, Computers and Structures 69 (1998) 197-208

J. Li, R. Shen, H. Hua and X. Jin, Bending-torsional coupled vibration of axially loaded composite Timoshenko thin-walled beam with closed cross-section, Composite Structures, 64 (2004) 23-35

# Text boxes

Second Mode Shapes

First Mode Shapes

ξ

ξ

ξ

Fourth Mode Shapes

Third Mode Shapes

ξ

ξ

ξ

1st Natural Frequency (Hz)

2nd Natural Frequency (Hz)

Force (N)

Force (N)

4th Natural Frequency (Hz)

Force (N)

3rd Natural Frequency (Hz)

Force (N)