FLEXURAL–TORSIONAL COUPLED VIBRATION ANALYSIS OF A ROTATING CLOSED SECTION COMPOSITE TIMOSHENKO BEAM BY USING DTM

O. Ozdemir Ozgumus , M. O. Kaya Istanbul Technical University, Faculty of Aeronautics and Astronautics, Istanbul, Turkey

ABSTRACT

This study introduces the Differential Transform Method (DTM) to analyse the free vibration response of a rotating, closed section, composite, Timoshenko beam which features material coupling between flapwise bending and torsional vibrations due to ply orientation. The governing differential equations of motion are derived using Hamilton’s principle and solved by applying DTM. The natural frequencies are calculated and the effects of the bending-torsion coupling, the slenderness ratio and several other parameters on the natural frequencies are investigated using the computer package, Mathematica. Wherever possible, comparisons are made with the studies in open literature.

COMPOSITE BEAM MODEL

A straight composite beam with length , height  and breadth  is shown in Fig. 1. In the right-handed Cartesian coordinate system, the -axis is the centroidal axis of the beam. The flapwise displacement,  and the torsional rotation,  occur about the -axis and the -axis, respectively. Here,  and , respectively denote the spanwise coordinate and the time. The beam rotates with a constant angular velocity, . Since the cross-sections of the beam have symmetry in both planes, the -axis is also the locus of the geometric shear centers of the beam cross-sections. Therefore, the beam features material coupling between flapwise bending and torsional vibrations only due to ply orientation.

Figure 1. Configuration of a Uniform, Rotating, Composite, Timoshenko Beam

FORMULATION

Potential and Kinetic Energy Expressions

The total potential energy expression,  is given by Ref.[1] and derivation of the kinetic energy expression,  is made in this study. As a result, the following expressions are obtained for a rotating, composite Timoshenko beam

(1a)

(1b)

where primes and dots denote differentiation with respect to spanwise coordinate  and time , respectively. Here  is the material density;  is the cross sectional area;  is the mass per unit length,  and  are the second moments of inertia of the beam cross section about the  and  axes respectively;  is the polar mass moment of inertia per unit length about the  axis; , ,  and  are the flapwise bending rigidity, torsional rigidity, bending–torsion coupling rigidity and shear rigidity of the composite beam, respectively.

Governing Equations of Motion

The governing differential equations of motion and the associated boundary conditions are obtained applying the Hamilton’s principle to the energy expressions given by Eqs. (1a) and (1b).

Equations of motion:

(2a)

(2b)

(2c)

where  is the centrifugal force that is given by

(3)

Boundary Conditions:

- The geometric boundary conditions at the cantilever end, , of the composite beam,

(4a)

- The natural boundary conditions at the free end, , of the composite beam,

Bending moment:								            (4b)

Shear force:								            (4c)

Torque:								            (4d)

Exponential Solution and Dimensionless Equations of Motion

A sinusoidal variation of ,  and  with a circular natural frequency  is assumed and the functions are approximated as exponential solutions.

,   	   ,   				              (5)

Additionally, the following dimensionless parameters are used to be able make comparisons with the studies in open literature

,      ,   ,    							              (6)

Substituting Eq.(5) into Eqs.(1a)-(1c) and using the dimensionless parameters, equations of motion can be rewritten as follows

(7a)

(7b)

(7c)

where the dimensionless coefficients are

,      ,

,   								            (8a)

,      ,      ,   			            (8b)

,      ,      ,

(8c)

APPLICATION OF THE DIFFERENTIAL TRANSFORM METHOD

The Differential Transform Method is a transformation technique based on the Taylor series expansion and it is a useful tool to obtain analytical solutions of the differential equations. In this method, certain transformation rules are applied and the governing differential equations and the boundary conditions of the system are transformed into a set of algebraic equations in terms of the differential transforms of the original functions and the solution of these algebraic equations gives the desired solution of the problem with great accuracy. The application procedure of this method can be found in Ref.[2]. Applying the Differential

Transform Method to Eqs. (7a)-(7b), the following transformed equations of motion are obtained.

(9a)

(9b)

(9c)

where ,  and  are the transformed functions of , , , respectively.

Additionally, transformed boundary conditions are obtained as follows by applying DTM to Eqs.(4a)–(4d)

at           							          (10a)

at             					          (10b)

(10c)

(10d)

RESULTS AND DISCUSSIONS

The computer package Mathematica is used to write a program for the expressions given by Eqs.(9a)-(10d). In order to validate the computed results, an illustrative example that studies a nonrotating composite Timoshenko beam is taken from Ref. [3] is solved by using the formulas given above. When the results are compared with the ones given in Ref. [3], it is seen that there is a very good agreement between the results. Additionally, effect of the rotation speed on the natural frequencies is examined and the related graphic is plotted.

The beam model that is studied in Ref.[3] is a uniform, nonrotating, cantilever glass-epoxy composite beam with a rectangular cross section with width = 12.7 mm and thickness = 3.18 mm. Unidirectional plies each having fiber angles of are used in the analysis. The data used for the analysis are as follows:

In Table 1, the calculated results are compared with the ones given by Ref. [2] and a vewry good agreement is observed.

Table 1. Validation of the Calculated Results

| Natural Frequencies |
| --- |
| DTM | Ref.[3] |
| 30.7471 | 30.747 |
| 189.779 | 189.779 |
| 518.791 | 518.791 |
| 648.169 | 648.169 |
| 986.199 | 986.199 |
| 1564.75 | 1564.751 |

In Fig.2, mode shapes of a rotating composite Timoshenko beam are plotted.

In Table 2., effect of the rotational speed on the natural frequencies is given.

|  | Rotatinal Speed ( (rad / sec) |
| --- | --- |
|  | 0 | 50 | 100 | 150 | 200 | 250 | 300 |
| Natural Frequencies | 30.747 | 32.363 | 36.808 | 43.273 | 51.081 | 59.827 | 69.313 |
|  | 189.779 | 189.733 | 189.597 | 189.376 | 189.081 | 188.733 | 188.368 |
|  | 518.791 | 518.461 | 517.459 | 515.743 | 513.242 | 509.847 | 505.408 |
|  | 648.169 | 648.231 | 648.116 | 647.923 | 647.651 | 647.298 | 646.861 |
|  | 986.199 | 985.756 | 984.415 | 982.144 | 978.886 | 974.561 | 969.059 |
|  | 1564.751 | 1564.237 | 1562.684 | 1560.066 | 1556.335 | 1551.425 | 1545.248 |
|  | 1944.309 | 1944.231 | 1943.997 | 1943.604 | 1943.051 | 1942.334 | 1941.447 |
|  | 2241.307 | 2240.888 | 2239.557 | 2237.104 | 2233.289 | 2228.004 | 2221.298 |

References

[1] M. O. Kaya, O. Ozdemir Ozgumus, Flexural–Torsional Coupled Vibration Analysis of Axially Loaded Closed Section Composite Timoshenko Beam by Using DTM, Journal of Sound and Vibration, doi:10.1016/j.jsv.2007.05.049

[2] Ö. Özdemir, M.O. Kaya, Flapwise Bending Vibration Analysis of A Rotating Tapered Cantilevered Bernoulli-Euler Beam by Differential Transform Method, Journal of Sound and Vibration 289, 413–420, 2006..

[3] J. Li, R. Shen, H. Hua and X. Jin, Bending-torsional coupled vibration of  axially loaded composite Timoshenko thin-walled beam with closed cross-section, Composite Structures 64, 23-35, 2004.

# Footnotes

Research Assistant in Aeronautics Department, E-mail: ozdemirozg@itu.edu.tr

Associate Professor in Aeronautics Department, E-mail: kayam@itu.edu.tr

# Text boxes

(f)

(e)

(d)

(c)

Fourth Mode Shape

Second Mode Shape

Sixth Mode Shapes

Third Mode Shape

First Mode Shapes